Academic Lecture：Prof. A.Maazouz

Compounding and Melt strengthening of poly (lactic acid): Shear and elongation rheological investigations for forming process.

Abderrahim Maazouz

Université de Lyon, Ingénierie des Matériaux Polymères, IMP UMR CNRS #5223, INSA Lyon, 20 Avenue Albert Einstein, Groupe de Recherche pluridisciplinaire en Plasturgie/GRPP-INSA de LYON, France

Abstract-The poly (lactic acid) (PLA), through its organic origin and its biodegradation properties, can be a good alternative to petroleum-based polymers. To this end, the forming process as well blown extrusion and foaming of PLA was investigated in this study as an alternative for the production of food packaging. Through this work, we present some promising routes to enhance its processing ability which presents several challenges mainly due to the poor shear and elongation properties of this biopolymer. To our knowledge, there is no paper dedicated to the investigation of foaming and/or blown extrusion of PLA that involves structural, rheological and thermomechanical properties.

To achieve this objective, various formulations of PLA with multifunctionalized epoxy, nucleants and plasticizer were prepared and characterized on the basis of their linear viscoelasticity and extensional properties. The balance of chain extension and branching has been also investigated using solution viscosimetry, Steric exclusion chromatography (SEC) and rheology (relaxation spectrum, Van Gurp Palmen curves….). We pushed further by characterizing both the structure and thermomechanical properties of PLA formulations.

On one hand, a batch foaming assisted with supercritical CO2 was achieved following a full characterization in physicochemical, rheological and thermal domain, The influence of the foaming parameters, the extent of chain modification as well as the contribution of crystallization on cell morphology was evaluated. Based on these parameters, structures ranging from micro to macro-cellular-cell were obtained.

On the other hand, the stability maps of blown processing for neat and modified PLA were established at different die temperatures. We have achieved a great enhancement of the blown processing windows of PLA with high BUR (Blow Up Ratio) and TUR (Take Up Ratio) attained. We were able to demonstrate that a higher kinetic of crystallization can also be reached for chain-extended and branched PLA formulated with adequate amounts of nucleants and plasticizers. Induced crystallization during process was also demonstrated. Through this work, blown films with interesting thermomechanical and mechanical properties have been produced using an optimal formulation for PLA.

Keywords:  Poly (lactic acid), Rheology, Forming process, Chain extension and branching, Blown processing